## Slide 2
The Stripping Foil Test Stand in the Linac4 Transfer Line
W. Weterings
27th International Conference of the International Nuclear Target Development Society (INTDS-2014)
C. Bracco, R. Noulibos, Y. Sillanoli, P. van Trappen
CERN, European Organization for Nuclear Research, CH-1211 Geneva 23, Switzerland

## Slide 3: Talk Overview
Introduction
  LIU Project
  Linac4
  PSB Injection Region Configuration
Stripping Foil Test Stand
Layout & Instrumentation
Foil Handling Mechanism
Stripping Foil Specification
Test possibilities
Conclusion

## Slide 4: Introduction
LINAC 4
H−
LHC Injectors Upgrade (LIU) Project comprises a new Linac4, as well as major upgrades and renovations of the Proton Synchrotron Booster (PSB), the Proton Synchrotron (PS) and the Super Proton Synchrotron (SPS).
PSB
SPS
PS
LHC /
HL-LHC
Output energy
160 MeV
1.4 GeV
26 GeV
450 GeV
7 TeV
Linac2
50 MeV
Proton flux / Beam power
Present
Linac4
PSB
PS
2.0 GeV
LIU Project
The CERN Accelerator Complex

## Slide 5: Introduction
LINAC 4
H−
The 160 MeV H− beam from the Linac4 will be injected horizontally into the PSB by means of a H− charge exchange injection system, one for each ring.
The Linac4 project is a new 160 MeV H− linear accelerator replacing Linac2 as injector to the PS Booster (PSB).

## Slide 6: PSB Injection Region Configuration
The local orbit of the PSB beam is displaced by ~81 mm using two independent closed orbit bump systems:
The Injection Chicane, made by a set of 4 pulsed dipole magnets (BSW).
The Painting Bump, made by 4 horizontal kickers (KSW) outside the injection region, giving a 35 mm closed orbit bump, with falling amplitude.
A stripping foil will convert ~98% of the H− into protons by stripping off the electrons.
Configuration of the PSB injection region with 380mm long BSW magnets
Notes: Horizontal kickers (KSW), outside the injection region, produce 35 mm closed orbit bump.
Injection bump, BSW displaces beam by a constant 46 mm during the injection process.
1560-1032-380 = 148mm. Only ~130mm available for unit, narrow design

## Slide 7: Stripping Foil Test Stand
A stripping foil test stand will be installed in the Linac4 transfer line allowing tests with a 160 MeV H− Linac4 commissioning beam:
Testing from 2015, prior to final PSB installation (>2018)
The foil changing mechanism as well as the interlocking functions can be assessed;
Gain experience with these very fragile foils;
Test different foil materials and thicknesses;
Evaluate the lifetime of the foils and foil holders;
Measure the stripping efficiency and emittance growth of the beam through the stripping foil.

## Slide 8: Layout & Instrumentation
BCT + BLM
BCT
Profile Monitors
Stripping Foil
Test Stand Location
Source
DTL
CCDTL
PIMS
Dump
3 MeV
50 MeV
100 MeV
160 MeV
Linac4 Layout
Stripping efficiency is measured by current decrease between cross-calibrated Beam Current Transformers (BCT) and by taking the electrical signal from the foil holder.
Emittance growth is estimated using Secondary Electron Monitor (SEM) profile.
The upstream defocusing quadrupole (QD) is used to vary the beam size.
Transfer Line to PSB
Transfer Line
to PSB
QF
QD
Notes: QD from 2.5 T/m up to 9 T/m, the horizontal beam size (90%) can be varied from 2.5 mm to 3.7 mm respectively and the vertical beam size from 7.4 mm to 4.2 mm.
Beam can be transported to the main dump without any losses, provided that the downstream QF (L4T. MQF.0210) is switched off

## Slide 9: Foil Handling Mechanism
Rotating Belt
Foil Holder
Potentiometer
Conductive Ink
On Kapton®
Wipers
Micro
Switch
Foil movement of ±2mm, with a precision of ±0.1mm, from the nominal beam position.

## Slide 10: Foil Handling Mechanism
Stepping motor
UHV Magnetic coupling
Mirrors and
Optical Filters
Radiation Hard
Camera
Foil Changer
Beam Observation System (BTV) with
Screen in Beam
Rear View
Showing mirror
Notes: 1 mm thick Chromox (Al2O3 doped with CrO2) scintillating screen, engraved with calibration marks.
The BTV has a position accuracy of ±0.2 mm and for a large range of beam intensities remotely controlled optical filters are included.

## Slide 11: Foil Handling Mechanism
Stepping motor
UHV
Magnetic coupling
Mirrors and
Optical Filters
Radiation Hard
Camera
Foil Changer
Beam
Beam Observation System (BTV) with
Screen Retracted
Rear View
Showing mirror
Notes: A stripping foil current measurement will be made by means of taking the electrical signal from the foil holder

## Slide 12: Foil Handling Mechanism
Stepping motor
UHV
Magnetic coupling
Mirrors and
Optical Filters
Radiation Hard
Camera
Beam Observation System (BTV) with
Screen retracted
Foil Changer
Vacuum Chamber

## Slide 13: Foil Handling Mechanism
Final configuration to be
installed in Linac4
transfer line (L4T) sector 1.1

## Slide 14: Configuration L4T sector 1.1
To optimise intervention time and avoid foil damage due to differential pressure, the system is installed in a dedicated vacuum sector.
Vacuum
Valve
Vacuum Valve
Beam Current Transformer (BCT)
Stripping Foil Test Stand
Beam

## Slide 15: Stripping Foil Dimensions
The foil should be:
< 250 µg/cm2 to keep emittance growth below 0.1 π∙µrad, for the ~2 π∙µrad LHC beam.
< 200 µg/cm2 to keep uncontrolled beam loss below the 10-4 level.
> 150 µg/cm2 to ensure a theoretical stripping efficiency > 99 %.
Chosen baseline foil thickness 200 μg/cm2
The Stripping Foil Test Stand in the
Linac4 Transfer Line
H−, H0 and p+ yield at 160 MeV as a function of stripping foil thickness.
Notes: The stripping efficiency as a function of the carbon foil thickness was estimated by scaling the charge exchange cross-sections measured at 200 MeV to160 MeV [8].

## Slide 16: Stripping Foil Heating
The Stripping Foil Test Stand in the
Linac4 Transfer Line
Peak temperature on the 20 x 20mm centre area (left) and evolution of maximum temperature (right) in carbon foil for 1.3 x 1013 p+ beam injected at 1.2 s intervals. The equilibrium peak temperature is about 650 K.
Thermal foil damage is unlikely to be a foil lifetime or performance issue.
Notes: emittances around 8 and 6 π∙µrad are assumed in the horizontal and vertical planes
0.833 Hz, assuming only black-body radiation cooling

## Slide 17: Test possibilities
Stripping efficiency by measuring the BCT current before and after the foil (resolution of 0.1 mA).
Beam losses at the level of few 109 protons are expected for 1014 H− nominal intensity from L4.
A rough estimate of the emittance growth through the stripping foil could be obtained by using the SEM profile grids.
The PSB injection worst failure scenario can be simulated by hitting the foil with a 400 µs pulse and minimum beam size.
Many mechanical cycles and movement of the foil, with and without beam to test rigidity of different types of foils.
The BTV system will be tested, including correct filters selection for beam measurements over a large range of beam intensities as well as the Foil – BTV screen interference interlock.

## Slide 18: Conclusion
A stripping foil test stand in the Linac4 transfer line will allow testing of the foil exchange mechanism, controls, and instrumentation.
It will also allow measurement, at the % level, of the stripping efficiency for different foils.
A rough estimate of the emittance growth of the beam through the stripping foil can also be obtained.
The operation of the test stand will be in parallel with Linac4 operation and is anticipated to start autumn 2015.

## Slide 20: Spare Slides

## Slide 21: Spare Slides

## Slide 22: Spare Slides

## Slide 23: Spare Slides

## Slide 24: Spare Slides