## Slide 1: Low Cost Silicon Sensor
Y. Kwon
in exploration with
J. Lajoie, E. Kistenev, A. Sukhanov, and Z. Li
as part of MPC-EX R&D

## Slide 2: Si sensor in general
Mature technology
Reliable performance
Fine granule
Higher energy and time resolution (than gaseous ionization detectors)
Key burden is cost.

## Slide 4: Possibility in Korea
6 inch fabrication line
8 inch fabrication line
R&D environment
1 cm2 ~ $ 2

## Slide 5: ETRI/NNFC
ETRI
  Established PIN-type silicon sensor.
   = 0.4 , 6 inch line.
  Founded by government & self-sustaining for 6 years.
NNFC
  PIN-type sensor fabrication process needs establishment.
  SiPM fabrication.
   = 0.18 , 8 inch line (inefficient 4 & 6 inch support).
  Founded by government & government subsidy. terminated last year.

## Slide 6: Traditional Si sensor operation
-

## Slide 7: DC/AC coupled sensors

## Slide 8: Conventional AC-coupled sensor structure

## Slide 9: An implementation at ETRI

## Slide 10: How do we make it? (CMOS process)
High purity Si wafer
Oxidation
Ion implant
Oxide layer deposition
Etch for contact
Metal layer deposition
Passivation

## Slide 11: Actual process sheet

## Slide 12: Our collaboration model
Z. Li : Design/Process schematics
ETRI : Suggestion/Fabrication
A. Sukhanov : Coupling to electronics
Y. Kwon, E. Kistenev, J. Lajoie : Implementation, Quality control, follow-up, identification of main issues
Korean MPC-Ex groups : Test

## Slide 13: Structure with Al-overhang p+- implant, 20keV B, 1x1015/cm2

## Slide 14
n+ Implant (40 keV Ph, 1x1012/cm2) channel stopper added
n+ Implant (40 keV Ph, 1x1015/cm2)

## Slide 15: Nit=2E11/cm2; Bias: 200 V

## Slide 16: Mask layers (DC coupled sensor)
“p+”
“n+”
“contact”
“metal”
“passivation”

## Slide 17: “p+”

## Slide 18: “n+”

## Slide 19: “contact”

## Slide 20: “metal”

## Slide 21: “passivation”

## Slide 22: Processed Wafer

## Slide 23: Dicing
Key origin of trouble :
  Two sensors on one wafer
  When we use diamond saw (mechanical dicing), we have to use sticky tape to hold pieces still while in dicing. We couldn’t avoid exerting stresses to the sensor edges when we remove those sticky tapes after dicing.
Solution : Expander
  Dicing company suggested expander. No change in leakage current up to the bias of 3 x full depletion voltage.

## Slide 24: Where problems are …
~70 
~70 

## Slide 25: Expander

## Slide 26: After corrected procedure

## Slide 28: Photocurrent measurement (LED 1070 nm)

## Slide 29: Middle, 2V

## Slide 30: Middle, 8V

## Slide 31: Middle, 16V

## Slide 32: In-between, 2V

## Slide 33: In-between, 8V

## Slide 34: In-between, 16V

## Slide 35: In-between, 32V

## Slide 36: GR, 2V

## Slide 37: GR, 8V

## Slide 38: GR, 16V

## Slide 39: GR, 32V

## Slide 40: What is the issue? (1070 nm)

## Slide 41: Diffusion vs Drift
Very high resistivity
> 20 kcm
Lifetime
 > ms
e(h) thermal velocity :
2.3 (1.6) x 105 m/s
Charge collection by diffusion
when not by drift

## Slide 42: New efforts? (ALICE induced)
Readout ASIC
  Preamp + ADC + memory + trigger
  Built contact with CMOS image sensor expert.
  Running local MPW.
  KORIA might make some investment.
  Small scale funds might work… (Local grant application?)