## Slide 1: Introduction of the Progress in Detector Solenoids
Akira Yamamoto
KEK
Presented at sPHNIX held at RIKEN,
July 31, 2013

## Slide 2: Outline
Introduction
Accelerator Magnets
Detector Magnets
  Accelerator Experiments
  Space Experiments
Technical Topics
Summary

## Slide 3: Superconducting Magnets for LHC Experiments in Progress
ATLAS
(H. Ten Kate et al)
Alice (Resistive Coil)
D. Swoboda et al.,
LHCb (ResistiveCoil)
J. Andre, W. Flegel et al.,
CMS
(A. Herve et al)

## Slide 4
Superconducting Detector Magnets at LHC
Experiment B R E E/M Remark
[T] [m] [GJ] [kJ/kg]
ATLAS
CS 2.0(2.1) 1.25 0.04 7 (8.1) High-St. Al, no-cryo
Thin solenoid (0.7 Xo)
BT ~1 1.08 3 8 split, Largest
ET ~1 2x0.25 1.6 Single cold mass
CMS 4.0 3.2 2.6 12 Hybrid-conductor

## Slide 5: CMS: Solenoidal Field
Axial, Uniform Field
Self Supporting
Iron Return Yoke
Field inside the solenoid
  Sagitta measurement
  dp/p ~ {B • R2}-1
Deflection angle outside the solenoid
  dp/p ~ {B • R} -1

## Slide 6: CMS

## Slide 7: ATLAS: Toroidal Field
Self Closed Field
Field only at Detector Region
Field : proportional to R-1
6~ 8 coils in practical design
Largre field in the coil
Sophisticated support structure
to keep self balance
Saggita and deflection
  dp/p ~ {Bf•Ri • ln(Ri/Ro) / sin q }-1
q
Much Powerful Deflection in forward/backward direction

## Slide 8
width: 44m diameter: 22m weight: 7000t

## Slide 9: Central Solenoid
Thin coil
High-strength
Al-stabilizer
30 mm

## Slide 10: Features of Detector Magnets
Al-stabilized superconducting magnet
Indirectly cooled,
  forced flow 2-phase helium or
  thermo-syphon cooling

## Slide 11: Development of Detector Solenoid/Ring-Dipole Magnets
Experiment --Lab. B R (or L) X E/M Technical Remark (Year)
    [T] [m] [Xo] [kJ/kg]:
ISR CERN 1.5 1.1 Al-soldered to S/C (1977)
CELLO Saclay/DESY 1.5 0.85 0.6 Indirect cooling (1978)
*PEP4 LBL 1.5 1.1 0.83 Cu stab, in. Q-back (1983)
CDF Tsukuba/Fermi 1.5 1.5 0.84 5.4 Al co-extrusion (1984)
TOPAZ KEK 1.2 1.45 0.70 4.3 Inner coil winding, (1984)
VENUS KEK 0.75 1.75 0.52 2.8 CFRP vacuum shell, (1985)
AMY KEK 3 1..2 Hybrid of Cu/Al stab. (1985)
CLEO-II Cornell 1.5 1.55 2.5 3.7 Double layer (1988)
ALEPH Saclay/CERN 1.5 2.75 2.0 5.5 Thermo-siphon (1987)
DELPHI RAL/CERN 1.2 2.8 1.7 4.2 LHe-pump cooling (1988)
ZEUS INFN/DESY 1.8 1.5 0.9 5.5 Current grading, (1988)
H1 RAL/DESY 1.2 2.8 1.8 4.8 (1990)
BESS KEK 1.2 0.5 0.2 6.6 Thin-Al,Pure-Al strip (1990)
*CMD-2 BINP 1.2 0.36 0.38 5 Current shunting (1990)
G-2 BNL/KEK 1.5 6 One-ring dipole (1995)
WASA KEK/Uppsala 1.3 0.25 0.18 6 Thinnest (1996)
SDC-prt KEK/Fermi 1.5 (2) 1.85 1.2 9.6 High-st. Al, Isogrid (1993)
CLOE INFN (1997)
BABAR INFN/SLAC 1.5 1.5 (1997)
D0 Fermi* 2.0 0.6 0.9 3.7 Conforming of Al (1998)
BELLE KEK* 1.5 1.8 5.3 (1998)
ATLAS-CS 2 1.3 0.66 7 High St.Al-stabil. (2001)
(Blue is presently operated)

## Slide 12: Progress of Al-stabilized SC

## Slide 13
Recognized events;
Cello
Al-st. Thin..
Coil on mandrel
CDF
Al-co-extrusion,
TOPAZ
Inner winding
Aleph/Dephi
Thermo-syphone/Pump
Zeus/Cleo
Two layer, Grading
CMD
Res. Shunting (no insul.)
BESS/SDC
Pure-Al strip
SDC
High strength Al stab.
CMS
Hybrid conductor
BESS-P
Self supporting

## Slide 14
Support Cyl.
Bess-Polar
Self supporting coil
w/o outer sup. Cylinder

## Slide 15: Belle Solenoid for KEK B-Factory
KEK Site

## Slide 16: BELLE Coil Winding

## Slide 17: Roles of Aluminum Stabilizer
Stabilizer for Superconductor
  Low Resistivity, and high thermal conductance
Energy absorber with Joule Heating in case of quench
  Large heat capacity / mass
Transparency / Light weight
  Low Z, and low density
Mechanical Strength (to be improved)
  High-strength Aluminum Stabilizer

## Slide 18: Characteristics of Aluminum
Aluminum may provide very wide range characteristics
depending on the purity (or RRR)
Eletctical
Resistivity
Thermal
Conductivity
Al (RRR=1000)
Cu (RRR= 100)

## Slide 19: Two Approaches for High Strength Al Stabilizer
Reinforcement of Al
  with keeping low resistivity
Uniform reinforcement
  Micro-alloying and cold work
  ATLAS-CS
Hybrid reinforcement
  Welding Al-Alloy with pure-Al
  CMS
Hybrid
Uniform
Alloy / Pure-Al / Alloy
Uniform Micro-alloying
NbTi/Cu

## Slide 20: Micro-alloying with pure-Al
Additve metal A Dens. Solubility Resistivity contribution
(in solution / crystal.)
[g/cm3] [w-%] [10-12 Wm/wppm]
Solid solution:
Si 28 2.6 1.65 0.7 0.088
Zn 65 7.1 83 @ 400C 0.10 0.023
Crystallization / Precipitation:
Ni 59 8.8 0.05 @640C 0.81 0.061
<0.006 @<500C
Ni: Best reinforcement with keeping Low resistivity.

## Slide 21
Al3Ni precipitated
Contributes as
structural component
Pure-Al region
Keep low resistivity
Ni>> High
0.1%
0.5%
Composite structure formed by
Micro-alloying and precipitation

## Slide 22
High-strength Al-stabilizer
Micro-alloying + Cold-work (area rediction) hardening
Ni 0.1 ~ 2 % + 15~20 % Cold-work

## Slide 23: CMS with Hybrid Structure (5N-Al/AA6082)
Overall mechanical strength
Y.S . :
130 MPa @ 300 K before curing
180 MPa @ 300 K after curing
(258 MPa @ 4.2 K, estimated)
Electrical properties of inserts
RRR :
3020 @ 0 T
1134 @ 1 T
977 @ 5 T
B. Cure, B. Blau. A. Herve, et al, this conference

## Slide 24: Comparison with Cu and Al Alloy
Al-stabilized superconductor becoming equivalent to or
stronger than ordinal Cu stabilized superconductor
effectively

## Slide 25: Progress of Al-stabilized SC

## Slide 26: Energy / Mass Ratio
Magnetic Field: rot B = µ0J
Stored Energy: E = 1/2µ0 ∫ B2 dv
Coil Mass: M = Vcoil  g
Pressure: p = B2/2µ0
Hoop Stress: shoop = (R/t) • p
Wall thickness: t = (R/sh) • p
E/M ratio: E/M = (B2/2µ0) • R/2g
= sh/2g
B: magnetic field
µ0: permeability
Vfield: magnetic volume
Vcoil: coil volume
g: effective density
shoop: hoop stress
R: coil radius
t: coil thickness

## Slide 27: E/M Ratio Energy Density to Coil Mass = Temperature Rise after Quench (all energy dump)
Enthalpy
H = E/M = Int. Cp dt
---------------------------------
20 kJ/kg ~100 K
10 kJ/kg ~ 80 K
5 kJ/kg ~ 65 K
---------------------------------
Temp [K]
Correspond to:
Peak Temperature with homogeneous energy dump
80, 100 K
Thermal
Expansion
Entharpy

## Slide 28: Safety against Quench
Energy extraction (CMS)
  ~ Half energy to be extructed
    E/M = 12 kJ/kg >> effectively 6 kJ/kg
Full energy absorption (ATLAS)
  Using quench back techniques such as
  Quench Protection Heater (BT, ET, CS)
  Pure-Al strips and QPH (ATLAS-CS)

## Slide 29: Progress in E/M Ratio in Detector Magnets
Reached

## Slide 30: Wall Thickness / Material
Magnetic Field: rot B = µ0J
Stored Energy: E = 1/2µ0 ∫ B2 dv
Coil Mass: M = Vcoil  g
Pressure: p = B2/2µ0
Hoop Stress: shoop = (R/t) • p
Wall thickness: t = (R/sh) • p = (R/sh) • B2/2µ0
E/M ratio: E/M = (B2/2µ0) • R/2g
= sh/2g
B: magnetic field
µ0: permeability
Vfield: magnetic volume
Vcoil: coil volume
g: effective density
shoop: hoop stress
R: coil radius
t: coil thickness