## Slide 1: CNS CVD Diamond
S. Michimasa

## Slide 2: Properties of diamond
Extreme mechanical hardness and extreme high thermal conductivity
  Broad optical transparency in region from IR to UV
    Insensitive for visible light
  Diamond is a semiconductor (band gap = 5.47eV) and very high resistivity at room temperature (1016Wcm)
    No cooling and No p-n junction ⇒ Easy operation
  High charge carrier mobility (e: 2200/h: 1600 cm2/Vs)
    Fast rise time of detector signal
  High energy needed to remove carbon atom from the lattice (80 eV)
    Radiation hardness

## Slide 3: Accessibility for diamond detector
Diamonds materials (commercially)
  Single-crystal CVD diamond plate
    Maximum size: 5×5 mm2, d=50,100,200,300mm (commercially)
  Polycrystalline CVD diamond plate
    Maximum size: 50×50 mm2, d=50,100,200,300mm (commercially)
Development of large size of Polycrystalline CVD DD
  Beam spot size : typically 20×20 mm2 at the BigrRIPS-F3 achromatic focus ⇒ pCVD diamond can cover achromatic beam spots of BigRIPS.
  Signal size is determined by energy loss in the detector: ⇒ dE/dx ～ 100 keV/mm ～ 105 e-h/mm (12N 250A MeV) Sufficient number of e-h pair can generate a clear pulse signal. ⇒ Heavier ions are more promising.

## Slide 4: CNS diamond detectors
Signals for 32-MeV 4He beam
= Energy loss equivalent for 250-MeV/u 14N
Side A
Side B
Side B (another side of blue)
Specification
Effective Area: 28 mm□
Thickness: 200um
Number 3 pieces
Time resolution 30 ps (s)
Ref: S.Michimasa NIM B 317 (2013) 710.

## Slide 5: Typical electric circuit
Circuit is very simple.
Care about high-frequency cables and circuits
For High-rate capability, following changes will be efficient.
TDC → Multi-hit TDC.
QDC → Time-over-Threshold + Multi-hit TDC.
inverter

## Slide 6: Preliminary result for Xe beam (1)
Detector Setup (at HIMAC)
Beam Condition: 124Xe at 95A MeV, 1M-3M ppp ※ Preamplifier is the same for light ions (14N) E loss in Dia.: 124Xe/14N = 2091.4/18.5 = 113
Outputs (by Oscilloscope)
Dias #1 and #2 are almost completely coincidence.
⇒ Efficiency for Xe beam are almost 100% .
Preamp output is frequently saturated but logic signals are correctly generated. ⇒ Beam intensity up to a few MHz will be countable.
20ns

## Slide 7: Preliminary result for Xe beam (2)
Irradiation test of 1 Mppp
Detector Setup (at HIMAC)
Period : 5 hours Beam intensity: 1M-3M ppp (count by Plastic)
Plastic scintillator:
Pulse height is reduced 1/2 - 1/3 from the initial status.
Surely underestimate left-shown beam intensity.
Burnt spot by beam.
Diamond Detectors:
Pulse height is not changed from the initial status.
Leak current was increasing with irradiation (up to 15 uA). (Leak current without beam was 15nA. We do not know how much is limit for operation…)

## Slide 8: Next step and target experiment
Longer-time irradiation (at least 1 day)
  Simulation of BigRIPS condition.
    Atomic number, Beam size, Beam energy, Intensity
CNS develops diamond detector for the 132Sn(d,d’) experiment (Spokes person: S.Ota).

## Slide 9: If You hope further information on a CNS diamond detector.
Contact to
S. Michimasa (mitimasa@cns.s.u-tokyo.ac.jp)