## Slide 1: Recent spallation materials researches performed at PSI
HPTW2023, RIKEN, Japan 06.11.2023
Yong Dai, Peng Bi, Peng Song (PSI), Hossein Sina, Michael Wohlmuther (ESS)

## Slide 2
Content
PIE of target material: Tungsten
PIE of proton beam window (PBW) materials: Inconel 718 & Al-6061

## Slide 3
PIE of target material: Tungsten
Revision of irradiation parameters based on gamma measurements
Protons

## Slide 4
PIE of target material: Tungsten
3-point bend test
Thermal diffusivity measurement
Details in Sina Hossein’s talk on Thursday

## Slide 5
PIE of target material: Tungsten
Atom probe tomography (APT)
In neutron irradiation: mainly Re and Os (can be much higher! 1% at / dpa)
20nm × 20nm × 5nm Slice
6.4 dpa
As Received
28 dpa
Clear clustering of Re in irradiated samples
Clustering of other Transmutants not clear, due to low concentration

## Slide 6
PBW materials
PBW of ESS: Al-6061-T6
PBW of SNS: SA Inconel 718
PBW of LANSCE: PH Inconel 718
2.3 mm wall thickness, Max. dose 20 dpa
PBW of SINQ: AlMg3
2.0 mm wall thickness, Max. p-fluence: 8.6x1025 p/m2 Max. dose 8.5 dpa
1.8/2.0 mm wall thickness, Max. dose 20 dpa
McClintock, Acta Mater. 231 (2022) 117889
James, JNM 296 (2001) 139

## Slide 7
PH Inconel 718 irradiated at LANSCE
Max. 3.0 x 1025 p/m2, ~10 dpa, <400°C
Irradiated with 800 MeV / 1 mA protons for 9 months during 1995 – 1997. A leak was detected after 6 months.
PIE of PBW material: Inconel 718
SA Inconel 718 irradiated at SNS
James, JNM 296 (2001) 139
Max. 9.7 dpa, 110°C
PBW-4 was operated for 2 years, with 940 MeV protons and 8674 MWh.
5- 9.7 dpa
3- 5 dpa
McClintock, Acta Mater. 231 (2022) 117889

## Slide 8
Inconel 718 irradiated in STIP-II
Maloy, JNM 417 (2011) 1005.
protons
SINQ Target Irradiation Program – STIP
Inc. 718 SPF
PIE of PBW material: Inconel 718

## Slide 9
Inconel 718 irradiated in STIP-II
McClintock’s data range
PIE of PBW material: Inconel 718

## Slide 10
Inconel 718 irradiated in STIP-II
PIE of PBW material: Inconel 718

## Slide 11
Inconel 718 irradiated in STIP-II
PIE of PBW material: Inconel 718
HV0.2Ann=220
HV0.2CW= 459
Chen, JNM 343 (2005) 236

## Slide 12
Proton fluence: 8.5x1025 /m2
8.8 dpa / 2400 appm He / 4800 appm H
Al-alloy: AlMg3
Al-alloys for PBW applications
SINQ Target-3 (1998-99), 6.8 Ah P+
SINQ Target-9 (2011-12), 13.13Ah P+
SINQ Target-4 (2000-01), 10.03 Ah P+

## Slide 13
Al-alloy: Al 6061-T6
Al-alloys for PBW applications
Irradiation in STIP-7 (Target-10, 2013-14)
to be published
R4
n-flu. | 9.5x1025/m2
p-flu. | 1.6x1025/m2
Dose | 10.1 dpa
He | 455 appm
H | 1095 appm
Tirr | 62°C
to be finalized

## Slide 14
Al-alloy: Al 6061-T6
Tt=32°C
Tt=152°C
Microstructural results in Peng Song’s talk on Thursday
PIE of PBW material: Al 6061

## Slide 15: Thank you!