## Slide 1: Capabilities of the FLUKA particle transport code for the design of high-power targetry systems
C. Ahdida, F. Salvat Pujol and V. Vlachoudis on behalf of the FLUKA.CERN Collaboration

## Slide 2: Introduction to FLUKA

## Slide 3: Particle shower simulation
Radiation shower set up by a single 450 GeV/c proton in Al

## Slide 4: FLUKA
General-purpose code for the Monte-Carlo simulation of radiation transport
Maintained by the FLUKA.CERN Collaboration
Worldwide community of ~3000 active users
Mature simulation code: development started in the 1960s
Coupled hadronic/electromagnetic particle shower simulation
Over 60 particle species tracked, including γ, e±, μ±, 𝜏±, 𝜈, hadrons, ions
Energy range:
  – up to 10 PeV
  – down to 100 eV for γ, 1 keV for e±/p, 10-14 GeV for n
Not a simulation toolkit: most reasonable physics models adopted on behalf of our users
Very few simulation parameters: transport/production thresholds, toggling exotic/time-consuming processes, etc
Combinatorial geometry package for arbitrarily complex geometries
Tracking in magnetic fields (and electric fields in vacuum)
Built-in variance reduction / biasing techniques
Built-in scoring capabilities for a broad variety of radiometric quantities

## Slide 5: FLUKA’s graphical user interface: Flair
Assists users in all simulation stages:
  Input setup
  Geometry definition, visualization & debugging
  Running (distributed)
  Processing output
  Visualizing results
https://flair.cern
Broad range of applications of FLUKA/Flair!
Constant evolution (e.g. planning RP interventions, animated movies)
E.g. energy deposition (GeV/cm3 in a test target at CERN’s H4IRRAD w/ 280 GeV/c mixed hadron beam)

## Slide 6: FLUKA features for high-power targetry design
Energy (dose) deposition
Secondary particle production
Radiation damage estimates
  DPA
  H and He production
Radiation to electronics
Prompt radiation and activation
  Prompt and delayed in a single run
  Radionuclide inventories
  Ambient doses (up-to-date fluence-to-dose conversion coefficients from ICRP116 and ICRU95)
Provides input for thermomechanical finite element analyses (ANSYS)

## Slide 7: Displacement damage observables in FLUKA

## Slide 8: DPA
The unit that is commonly used to link the “radiation damage effects” with “macroscopic structural damage” is the displacement per atoms
It is a “measure” of the amount of radiation damage in irradiated materials
3 DPA means each atom in the material has been displaced from its site within the structural lattice an average of 3 times
A quantity directly linked to the Non Ionizing Energy Losses (NIEL) but restricted in energy
DPA is a strong function of projectile type, energy and charge as well as material properties and can be induced by all particles in the cascade
However, DPA for the moment is a “mathematical” quantity that cannot be directly measured experimentally

## Slide 9: DPA in FLUKA
DPA-NRT and ARC-DPA
For all particle species
User-defined material constants barcdpa, carcdpa
During transport: restricted above the damage threshold
During ranging out (below 1 keV): unrestricted, relying on Lindhard partition function
Nordlund et al., Improving atomic displacement and replacement calculations with physically realistic damage Models, Nature Commun., 9:1084 (2018)
DPA-NRT
ARC-DPA
Nd – number of atomic displacements
Td – damage energy
Ed – average threshold displacement energy
Time-dependent evolution of displace-ment cascade based on molecular dynamics simulations

## Slide 10: BLIP tests
SS304 container with different capsules of material samples was irradiated at BLIP
Beam parameters:
  Proton E = 181 MeV
  sx,y = 5.1 mm
  1.03 · 1021 POT for High-Z I capsule
High-Z I capsule contained iridium, TZM and CuCrZr
High-Z I capsule
Joao Espadanal, Vasilis Vlachoudis
Beam distributions
TZM: (%) 99.273 Mo; 0.55 Ti, 0.12 Zr; 0.03 C; 0.01 Fe; 0.01 Si; 0.002 Ni; 0.002 N; 0.003 O
CuCrZr: (%) 98.76 Cu; 1.0 Cr; 0.15 Zr; 0.04 Fe; 0.05 Si
SS316
SS316
Panagraphite

## Slide 11: BLIP – Gas production per DPA
DPA is not the full picture for material damages
Other quantities should be considered, for instance the gas (H, He) production
In the BLIP example low energy protons are implanted in the material
If a large quantity of gas is produced and the material is not able to dissolve it in the inner structure, bubbles are created and cracks may appear
This may have a more important net effect than DPA itself → a factor of even 1000
Ir
TZM
CuCrZr
SS316
SS316
Panagraphite
Ir
TZM
CuCrZr
SS316
SS316
Panagraphite
DPA (ARC-DPA)
H production
0.4
0.2
0.2
0.2
0.1
max
Ir
TZM
CuCrZr
SS316
SS316
Panagraphite
Joao Espadanal, Vasilis Vlachoudis
Ir
TZM
CuCrZr
SS316
SS316
Panagraphite
0.2
H appm/DPA (ARC-DPA)
  1.03 · 1021 POT

## Slide 12: Application: radiation damage in the Muon Collider arc

## Slide 13: Muon collider: shielding study for dipole arc magnets
Geometry
Parameters
Calzolari et al., IPAC2022 doi:10.18429/JACoW-IPAC2022-WEPOST001
3 cm-thick W
Similar power dissipated by decay e-/e+ due to diff. ring circumference
Generic study with string of conventional dipole magnets (6 m long) and 20 cm long drift regions in between
IMCC aims to address key design questions for a multi-TeV muon collider
Multi-TeV muons still have a relatively short mean lifetime in the lab frame (0.1 s for √𝑠=10 ) and rapidly decay
The decay e-/e+ carry on average ~1/3 of the Eµ creating a dissipated power of several 100 W/m
Significant challenge for the collider design due to the instantaneous heat deposition and cumulative radiation damage
To sustain the radiation load, superconducting magnets need to be protected with a continuous absorber to
  prevent beam-induced quenches
  reduce the thermal load to the cryogenic system
  avoid magnet failures due to the cumulative dose in insulators and atomic displacements in superconductors

## Slide 14: Power, dose and DPA in superconducting coils
Short-term effects
Long-term effects
Calzolari et al., IPAC2022 doi:10.18429/JACoW-IPAC2022-WEPOST001
Peak power deposition in the coils
Maximum at around 1.2 and 1.5 mW/cm3 for 3 and 10 TeV, respectively
One order of magnitude smaller than the typical 15-20 mW/cm3 quench limit for the bending dipoles of the LHC
No problem in terms of magnet quenches
Dose over 10 y reaching 27 and 37 MGy is above customary limit
Additional shielding
More recent studies are within limits
DPA values reaching 10-4 over 10 years
Nb3Sn samples degrade above 10-3 DPA
Similar DPA in inner triplet magnets for HL-LHC after 3000 fb-1
DPA expected to be fine

## Slide 15: Application: neutron attenuation benchmark

## Slide 16: Neutron attenuation benchmark
A benchmark facility for testing different shielding material and thicknesses in comparisons of measurements and MC simulations
CERN Shielding Benchmark Facility (CSBF)
Nakao et al., Measurement and simulations of high-energy neutrons through a various thickness of concrete and steel shields using activation detectors at CHARM and CSBF, Journal of Nuclear Science and Technology
5x1011 p/pulse 24 GeV/c
50 cm thick Cu, Al targets
Benchmarks are essential for providing adequate data for accelerators
Material samples (Bi, In, Al, C) were placed behind concrete and steel shielding of different thicknesses
Neutrons transmitted through the various shield settings were estimated by observing activation reactions
Attenuation profiles of radionuclides production rates

## Slide 17: FLUKA courses
Next FLUKA Beginner’s course will take place in April 2024 in Madrid
Stay tuned for any course announcements (FLUKA webpage & forum)

## Slide 18
Thank you very much for your attention!