## Slide 1
RaDIATE Collaboration Overview and Achievements in the Last Few Years on Materials
Frederique Pellemoine, on behalf of the RaDIATE Collaboration
8th HPTW – November 6-10, 2023 - RIKEN, Japan
7 November 2023

## Slide 2: Outline
Introduction
  High Power Targetry Context
  Common challenges in beam intercepting devices
RaDIATE Collaboration
  Common interest
RaDIATE program and approach
  Current research approach and results
    In-beam studies
    Develop alternative methods
    Novel materials development
    Develop modeling
Summary

## Slide 3: High Power Targetry Context
Beam Intercepting Devices (BIDs) are continuously bombarded by high-energy high-intensity particle beams
  Primary beam and target containment windows
  Secondary particle-production targets (eg. neutrino targets)
  Collimators, Absorbers
Few target examples
  Neutrino production at Fermilab National Accelerator Laboratory
    graphite target
    ~ 1MW of 120 GeV pulsed proton beam
    Future up to 2.4 MW
  Rare Isotope production at Facility for Rare Isotope beam (MSU-FRIB)
    graphite rotating target
    400 kW of heavy ion beams (from O to U) at a minimum of 200 MeV/u
  Neutron production at Oak Ridge National Laboratory (Spallation Neutron Source)
    Liquid mercury target
    1.4 to 2 MW of 1.3 GeV pulsed proton beam

## Slide 4: Challenges associated with BIDs
Radiation Damage: Displacements in crystal lattice expressed as Displacements Per Atom (DPA)
Hardening and embrittlement
Creep and swelling
Fracture toughness reduction
Thermal/electrical conductivity reduction
Coefficient of thermal expansion
Modulus of elasticity
Transmutation products (H, He gas production can cause void formation and embrittlement)
Thermal Shock: Sudden energy deposition from pulsed beam
Fast expansion of the material surrounded by cooler material generates localized area of compressive stress
  1 MW target: ~250 K in 10 µs pulse (2.5 x 107 K/s)
Stress waves move through the material at sonic velocities. Plastic deformation, cracking and fatigue failure can occur
Thermal Fatigue: Cycling loading environment
Cycling loading progressively damage material’s microstructure such that it can ultimately fail at stress levels that are actually lower than its failure strength
D.L. Porter and F. A. Garner, J. Nuclear Materials, 159, p. 114 (1988)
Iridium (left) and Sigraflex (right) targets tested at CERN’s HiRadMat facility
Horn stripline fatigue failure (FNAL)

## Slide 5
R a D I A T E Collaboration
Radiation Damage In Accelerator Target Environments
RaDIATE collaboration created in 2012, with Fermilab as the leading institution. The collaboration has grown up to 20 institutions over the years.
First MoU was signed with 5 institutions 10 years ago!
Objective:
Harness existing expertise in nuclear materials and accelerator targets
Generate new and useful materials data for application within the accelerator and fission/fusion communities
Activities include:
Analysis of materials taken from existing beamline as well as new irradiations of candidate target materials at low and high energy beam facilities
In-beam thermal shock experiments
Contact:
Frederique Pellemoine, fpellemo@fnal.gov
Web: radiate.fnal.gov
Notes: To address these material challenges, the HPT community formed the RaDIATE collaboration in 2012, with Fermilab as the leading institution. The goal was to bring experts from the accelerator and fission/fusion communities together to generate new data for accelerator materials. The collaboration has grown up to 14 institutions over the years.

## Slide 6
R a D I A T E Collaboration
Radiation Damage In Accelerator Target Environments
Facility/Accelerator
Irradiation station
Post Irradiation Examination

## Slide 7
R a D I A T E Collaboration
Radiation Damage In Accelerator Target Environments

## Slide 8: High-Power Targetry R&D Approach
In-Beam Studies
Evaluate in-beam performance of candidate materials
Irradiated Material Studies: high energy proton irradiation at BNL-BLIP
Thermal shock testing: HiRadMat facility at CERN
Alternative Methods
Emulate high energy proton irradiations for accelerated and cost-effective material screening
Low Energy Ion: for assessing radiation damage effects
Electron beam for thermal shock and fatigue testing
Novel Testing Methods (fatigue studies)
Novel Target Materials
New materials with enhanced thermal shock and radiation damage resistance
High-Entropy Alloys
Nanofibers
Composite materials
Heat treatment
Develop Modeling
Prediction of fundamental response of various materials to irradiation and thermal shock
Helium gas bubbles formation and segregation
Radiation damage effects
Heat transfer mechanism in nanofiber media

## Slide 9: High-Power Targetry R&D Approaches
In-Beam Studies
Evaluate in-beam performance of candidate materials
Irradiated Material Studies
  From failed/used devices
  From high energy proton irradiation at BNL-BLIP
Post-Irradiation Examination
Thermal shock testing
  HiRadMat facility at CERN
High-energy proton irradiation
Post-Irradiation Examination
In-beam thermal shock
2017-2018
2015 2018 2022
E. Wakai - talk 100 - Tuesday
D. Kim - poster 17 - Tuesday
A. Casella - poster 20 - Tuesday
D. McClintock - talk 95 - Thursday
S. Meigo - talk 100 - Tuesday
F. Boix Pamies – talk 42 - Monday

## Slide 10: Future HiRadMat Experiment
Previous HiRadMat experiment (2015, 2018 and 2022)
  Understand and compare single-shot thermal shock response and limits between non-irradiated and previously irradiated material specimens from BNL BLIP
  Explore various materials: different grades of conventional materials, novel materials
  Directly measure beam-induced dynamic effects to validate simulation codes
Preparing a proposal for beam in 2025
  Use beam induced stress wave to estimate dynamic fracture toughness of target materials
    Static stress intensity factor
    Stress wave Dynamic loading
      Stress field around crack tip is not in equilibrium and inertia effects can not be neglected
      Crack may propagate instantly depending on magnitude of stress wave and rate at which it is applied
LDV /gage location to detect change in crack growth

## Slide 11: High-Power Targetry R&D Approaches
Alternative Methods
Emulate high energy proton irradiations for accelerated and cost-effective material screening
To thermal shock
  Electron/laser beam for thermal shock and fatigue testing
To Radiation damage
  Low Energy Ion: for assessing radiation damage effects
To High-Cycle Fatigue Testing
  Novel Testing Methods (fatigue studies)
R. Cowan - poster 20 - Tuesday
S. Bidhar - talk 66 - Wednesday
E. Wakai - talk 100 - Tuesday

## Slide 12: High-Power Targetry R&D Approaches
Novel Target Materials
New materials with enhanced thermal shock and radiation damage resistance
High-Entropy Alloys
Nanofibers
SiC-coated graphite and SiC-SiC composites
Dual-Phase titanium alloys
Toughened Fine-Grained Recrystallized (TFGR) Tungsten
Advanced graphitic materials
K. Ammigan - talk 36 - Tuesday
A. Burleigh - poster 18 - Tuesday
S. Makimura - poster 21 - Tuesday
Looking beyond conventional materials
Novel materials to enable next-generation multi-MW accelerator facilities
https://arxiv.org/abs/2203.08357
HEP High Power Targetry Roadmap Workshop – Targets and Sources (April 11-12, 2023)
https://indico.fnal.gov/event/59123/
E. Wakai - talk 100 - Tuesday

## Slide 13: High-Power Targetry R&D Approaches
Develop Modeling
Prediction of fundamental response of various materials to irradiation
Helium gas bubbles formation and segregation
Radiation damage
  dpa
  in Ti-alloys
  In HEAs
Heat transfer mechanism in nanofiber media
D. Senor - invited talk 97 - Monday
S. Meigo - talk 22 - Monday
G. Arora - talk 47 - Tuesday
A Roy et al., J. Nuclear Materials 586 (2023) 154695
H. Matsuda, JNST 57 1141 (2020)
S. Meigo, EPJ Web of conf 239 06006 (2020)

## Slide 14: R&D Related to RaDIATE Collaboration
Neutrino Production
Muon Production – US
Rare Isotope Production
Neutron Production
Cooling System
Muon Production – Japan
Q. Peterson - talk 96 - Thursday
J. Song - talk 28 - Friday
Y. Fukao - talk 112 - Monday
K. Yonehara – talk 133 - Tuesday
Z. Liu - talk 64 - Wednesday
N. Kamei - talk 99 - Tuesday
S. Makimura - talk 45 - Wednesday
S. Matoba - talk 114 - Thursday
N. Kawamura - poster 14 - Tuesday
H. Sunagawa - poster 15 - Tuesday
T. Sakamoto - poster 21 - Tuesday
S. Makimura - poster 22 - Tuesday
Y. Nagasawa - poster 23 - Tuesday
M. Ooi - poster 24 - Tuesday
P. Hurh - talk 52 - Thursday
J. Maestre - talk 35 - Tuesday

## Slide 15: Summary
Future high-power beams present critical target facility challenges
  Understanding material behavior under intense multi-MW beams
Materials R&D is essential to help design robust targetry components and maximize primary beam power on target and secondary particle production
Globally coordinated R&D activities through the RaDIATE Collaboration are producing useful results
  In-Beam irradiation for prototypic irradiation to closely replicate material behavior in accelerator target facilities
  Develop alternative irradiation facilities, material testing and characterization methods to have effective (cost and time) support to R&D program
  Look beyond the conventional materials and explore novel material
  Develop advanced modeling to better understand and predict fundamental response of various materials to irradiation

## Slide 16: Thank you for your attention
radiate.fnal.gov

## Slide 17: Backup Slides

## Slide 18: Analysis and Mitigation of Thermal Issues in a Nanofiber Target
W. Azstalos and Prof. Y. Torun (IIT)
Need better understanding of mass and heat transport mechanism in nanofiber media
Low packing density samples survived
Holes, cracks in higher density samples
Beam
Very complex heat and mass transfer
Conduction along fiber axis and crossings
Convection through He flow
Radiation reflects off nearby fibers, additional heating at certain λ’s
Need of nanoscale radiation model (λ-r)
Complex fluid flow
Low packing density
High packing density
Use Porous Media Models to handle all three modes of heat transfer:
Conduction: introduce effective k(T) for nanofiber mat due to Bhattacharyya and Daryabeigi
Convection: use Darcy’s Law to simulate fluid flow, include energy equation in simulations
Radiation: Mie Theory to solve scattering off infinite cylinder exactly, feed into model due to Lee
Approach:

## Slide 19: High Power Targetry Challenges
Heat removal
Thermal shock
Physics performance
Radiation damage
Operational safety
Storage and disposal
Thermal Shock and Radiation Damage were always identified as the most cross-cutting challenges of high-power target facilities but need to consider target thermal fatigue as fatigue stress cycle amplitude will be x2 at 2.4 MW
Notes: High power targetry community identified thermal shock and radiation damage as the most cross-cutting challenges facing HPT.

## Slide 20: Use Alternative to Understand Radiation Damage
HEP
HE protons
NE
neutrons
Irradiation stations
LE HI
e-
LE p
PIE Facilities
Modeling
Notes: We see synergy between the two communities where we can share techniques, facilities, expertise
Need experimental data to validate numerical models…

## Slide 21: High Power Targetry R&D Roadmap
HPT R&D is aligned with timeline of HEP Accelerators
HEP HPT R&D Workshop – April 11-12 2023