## Slide 1
Kavin Ammigan
8th High Power Targetry Workshop
6-10 November, 2023
Novel Materials R&D for Next-Generation Accelerator Target Facilities

## Slide 2: Motivation for Novel Targetry Materials
Advance the state-of-the-art in targetry materials for future multi-MW accelerators
  Enable the physics benefits of next-generation multi-MW accelerator target facilities
  Improve performance, reliability and operation lifetimes of beam-intercepting devices
Neutrino HPT R&D Materials Exploratory Map
~10x increase in accumulated proton fluence and power density
LBNF/DUNE 2.4 MW
Mu2e-II
Future Muon Collider and Neutrino Factory (4 MW+)
MINOS NT-02 target failure: radiation-induced swelling (FNAL)
Primary Be window embrittlement (FNAL)

## Slide 3: Looking Beyond Conventional Materials
Radiation Damage
Nanocrystalline materials: fine grains with high-density grain boundaries
  GBs serve as defect sinks to absorb and annihilate irradiation-induced defects
Phase stability
  Prevents irradiation-induced grain coarsening and void swelling
Other inherent irradiation resistance properties
Thermal Shock
Reduce stress magnitude, stress wave velocity and fatigue life
Low density
Low elastic modulus
Low coefficient of thermal expansion
High specific heat
Inherent ability to absorb and dampen stress waves
Exploit the inherent properties of High-Entropy Alloys (HEAs) and Nanofiber materials, two promising novel classes of materials for accelerator target applications
HEAs for beam window applications
Nanofibers for particle production targets

## Slide 4: High-Entropy Alloys
HEAs are alloys with multiple principal elements
Equi-atomic or near equi-atomic composition
Usually defined as being primarily a solid-solution matrix
Distorted lattice
Large composition space to explore new materials
High-temperature strength
High specific strength
Improved fatigue and fracture properties
Corrosion and oxidation resistance
Enhanced radiation tolerance
  Greater phonon scattering, sluggish diffusion of atoms/defects, broad migration energies, and more…
Promising properties observed
Swelling of increasingly complex alloys under ion irradiation, Jin et al., Scripta Materialia 119 (2016)
Void swelling shown to be less pronounced in more compositionally complex alloys upon heavy-ion irradiation (3-MeV Ni+ ions to 5 x 1016 cm-2 at 773 K), Lu et al., Nature Com., 2016

## Slide 5: HEAs for Accelerator Beam Windows
Elemental selection considerations
Light-weight elements (low density)
  Reduced interaction with protons
  Minimize energy loss and multiple scattering
Primarily a single-phase alloy
  Better ductility and manufacturability
Minimal activation
  Safer/easier to handle and dispose after use
Equimolar Cr-Mn-V shown to be single-phase BCC
Ti additions reduce concentration of interstitial impurities by forming Ti-(C,O,N)
Concerns Ti concentrations above ~8% will promote Laves phase formation
Fe forms intermetallic compounds near the equimolar ratio with Cr, Ti, V
Most commonly used elements in HEAs from literature (Miracle, 2017)
Common alloys: CoCrFeMnNi (Cantor alloy), AlxCoCrFeNi, AlxCoCrCuFeNi

## Slide 6: HEA Design Approach
CrMnV
Equimolar BCC single phase
CrMnTiV
Impurity getter
AlCrMnTiV
BCC phase stabilizer
AlCoCrMnTiV
Semi-coherent secondary phase
CALPHAD simulations to understand the thermodynamics and phase diagrams of the multicomponent alloy systems
Goals
Broaden BCC phase field range
Reduce Laves phase formation temperature
Lower density
Add semi-coherent precipitates (B2 phase)

## Slide 7: Preliminary HEA Synthesis
Sectioned arc-melted ingots (UW-Madison)
HEA samples sealed in quartz under vacuum before heat treatment (UW-Madison)
4 HEA compositions
Cr33Mn33V33
Cr31Mn31Ti7V31
Al15Cr20Mn20Ti10V35
Al15Co4Cr25Mn15Ti6V35
Homogenized HEAs achieved target composition within 1at%
XRD confirmed BCC phase
A. Couet, M. Moorehead et al. UW-Madison

## Slide 8: HEA Plate Fabrication & Characterization
Procured plates from external vendor (Sophisticated Alloys Inc.)
  100 mm x 100 mm x 2 mm
  HIPed at 1200 ºC for 4 hr
  Homogenized at 1200 ºC for 48 hr
Microstructural characterization ongoing (SEM, EBSD, EDX, TEM, XRD)
SEM/EDX of Al15Co4Cr25Mn15Ti6V35
Ti(C-N)

## Slide 9: Hardness Measurements
No observable cracks at corners of indents
N. Crnkovich, UW-Madison
Relatively higher hardness than Ti but show promising signs of ductility
Modulus greater than Ti, but lower than Beryllium (303 GPa)
Lower density of Ti-(C,N)
Continuous stiffness measurements from nanoindentation work ongoing

## Slide 10: Density Functional Theory (DFT) calculations
Comparison of Young’s Modulus from DFT calculations with measurements
DFT (G. Arora, FNAL)
Measurements (N. Crnkovich, UW-Madison)
Cr33Mn33V33
Cr31Mn31Ti7V31
Al15Cr20Mn20Ti10V35
Al15Co4Cr25Mn15Ti6V35
Ti-6Al-4V
Building new inter-atomic potentials to study radiation damage effects in HEAs and guide compositions
G. Arora’s talk

## Slide 11: Initial In-Beam Tests
V2+ ion irradiation 50/100 DPA at 500 ºC at Wisconsin Ion Beam Laboratory
Two HEAs samples prepared for irradiation
TEM BF image of the irradiated cross-section
PIE starting…
What are the dominant irradiation effects?
Effects visible at low DPA?
Thermal shock test at CERN’s HiRadMat facility (2022)
HEA samples included in HRMT-60 RaDIATE experiment
Exposed to single-shot 7 × 1012 proton beam (𝜎 ~0.25 mm)
HEA samples images after beam pulse
PIE at UKAEA-MRF starting soon

## Slide 12: HEA Design Refinement & 2nd Gen. HEAs Synthesis
Systematic compositional space search using high-throughput CALPHAD simulations
  > 8,500 compositions (N. Crnkovich, UW-Madison)
  > 120,000 compositions (G. Arora, FNAL)
G. Arora’s talk
A. Burleigh’s poster
Al10Co4Cr25Mn26Ti1V34
Al10Co4Cr27Mn21Ti4V34
Al16Co2Cr25Mn30Ti1V26
Al16Co4Cr25Mn30Ti1V24
Al20Co1Mn27Ti2V50
Al12Co3Cr6Mn27Ti2V50
Al18Mn30Ti2V50
Al20Co2Mn26Ti2V50
Effect of Ti concentration as an impurity getter
Effect of Co as B2 phase enhancer
Effect of Al concentration and removing Cr
Effect of removing Co, with Al as the potential B2 phase enhancer
8 new HEA plates have been fabricated and currently being sectioned for analysis
To optimize BCC/B2 phase regions, onset of embrittling secondary phases, properties

## Slide 13: Electrospun Nanofiber Materials
SEM images of Zirconia nanofibers produced at Fermilab, (a) bulk nanofiber mat, (b) single nanofibers revealing polycrystalline grains (S. Bidhar)
Electrospinning technique and Taylor cone.
Intrinsically tolerant to both thermal shock and radiation damage
Nanofiber continuum is discretized at the microscale but continuum at meso-scale
  Reduced temperature gradient limited to fiber axis
  Fiber discontinuity mitigates stress wave propagation
  High surface area and gaps allow for effective local heat removal with gas
Evidence of radiation damage resistance due to nanopolycrystalline structure of ceramic nanofibers Bidhar et al., PRAB, 24, 2021
Photo: Reidar Hahn, FNAL

## Slide 14: In-Beam Tests of Ceramic Nanofibers
Ion irradiation (in-situ TEM)
Thermal shock test (HRMT-43) - 2018
TEM before irradiation
TEM after irradiation
@ Argonne IVEM Tandem, S. Bidhar, PRAB (24), 2021
1 MeV Kr2+ ion
3.25 x 1015 ions/cm2  5 dpa
No measurable change in lattice parameter
No defects formation
Evidence of radiation damage resistance
Low packing density
High packing density
440 GeV protons, σ: 0.25 mm, 1.21 x 1013 protons in 4 µs
Low packing density samples survived
Holes, crack in higher density samples

## Slide 15: Multiphysics Simulations of HRMT-43 Nanofiber Mats
Low packing density
High packing density
Pressure distribution at end of beam heating
Rapid heating of target  Pressure shockwave for a higher packing density target
Higher packing density reduces airflow induced by beam heating (natural convection) which exerts higher pressure on fibers
3D- fiber level simulation in progress
Bhattacharya model to evaluate effective thermal conductivity
MS & PhD work of Will Asztalos @IIT
2D mesoscale simulation (ANSYS FLUENT)

## Slide 16: Extending Work to Pure Tungsten Nanofibers
High temperature furnace with N2 gas flow
Heat treatment profile
W nanofiber mat after heat treatment
SEM/EDS show presence of Oxygen (~8-14 wt%) and Carbon
Increasing temperature during heat treatment reduced oxide formation to 1.35 wt%
  Will now heat treat with forming gas 5%H2+95%N2 to further reduce oxide
XRD analysis ongoing to evaluate crystal parameters, phase and structure
Investigating techniques to strip carbon from surface of fibers

## Slide 17: Materials Irradiation Screening
Michigan Ion Beam Laboratory (MIBL) with triple-beam irradiation capabilities
Wisconsin Ion Beam Laboratory (IBL)
A2D2 facility (FNAL)
Accelerated and cost-effective methods for screening and down-selecting candidate materials
  Low-energy ion irradiations
  Electron beam for thermal shock/fatigue
Pre/Post-irradiation material characterization
  Characterize size and density of radiation-induced dislocation loops, point defect clusters, void swelling and segregation (XRD, SEM/EDS, FIB/TEM, ..)
  Bulk property testing
A. Burleigh’s poster
S. Bidhar’s talk

## Slide 18: Prototypic Irradiations and Evaluation
Final phase: prototypic beam irradiation with high-energy high-intensity proton beams before final validation/evaluation (FOMs) and selection of novel materials
  BLIP facility at BNL, Fermilab beamlines or other facilities
  CERN’s HiRadMat facility
CERN’s HiRadMat facility for single-shot thermal shock tests
PNNL hot cells
D. Kim’s poster
A. Goillot’s talk

## Slide 19: Current Collaborations & Acknowledgements
Fermilab
K. Ammigan, G. Arora, S. Bidhar, A. Burleigh, F. Pellemoine
University of Wisconsin-Madison
A. Couet, N. Crnkovich, M. Moorehead, I. Szufarska
Illinois Institute of Technology
W. Asztalos, Y. Torun
The work was supported by Fermi National Accelerator Laboratory, managed and operated by Fermi Research Alliance, LLC under Contract No. DE-AC02-07CH11359 with the U.S. DOE. This material is based upon work supported by the U.S. Department of Energy, Office of Science, Office of High Energy Physics under an Early Career Research Program award to KA. This project has received funding from the European Union’s Horizon Europe Research and Innovation programme, under Grant Agreement No 101057511 (EURO-LABS)

## Slide 20: Summary
Innovate and advance state-of-the-art in targetry materials to support next-generation multi-MW accelerator target facilities
  High-Entropy Alloys (beam windows)
  Nanofiber Materials (secondary particle-production targets)
Iterative material development process
  Optimization of composition, microstructure and properties
  Planning several experiments (irradiations and material characterizations)
  Complementary DFT & MD modeling of radiation damage effects in HEAs
Potential benefit/impact
  Enable Fermilab’s multi-MW neutrino physics program (LBNF/DUNE 2.4 MW)
  Expand Fermilab’s accelerator R&D capabilities in HPT
  Benefits to international HEP and non-HEP programs

## Slide 21
Kavin Ammigan
8th High Power Targetry Workshop, Japan
6-10 November 2023
Novel Materials R&D for Next-Generation Accelerator Target Facilities