## Slide 1: DIFFUSION BONDING BY MEANS OF HIP FOR BEAM INTERCEPTING DEVICES AT CERN
A. Perillo Marcone, R. F. Ximenes, S. Pianese, F. X. Nuiry, M. Calviani, G. Arnau Izquierdo, J. Busom Descarrega, K.E. Buchanan, S. Sgobba, T. Coiffet, T. Weißgärber, T. Griesemer, I. Aviles Santillana, A. Gallifa Terricabras, A. T. Perez Fontenla, M. Cusworth, T. Dutilleul, W. Kyffin
08/11/2023

## Slide 2: Background
Several BIDs need to manage significant thermal power
“Efficient” and “quantifiable” thermal conductivity at the interface between different materials required
Some BIDs are meters long
Several BIDs are in UHV
    Many joining techniques are not compatible with UHV
    Welded connections/joints (water-vacuum barrier) inside vacuum are too risky

## Slide 3: Contact with cooling pipes – techniques used for BIDs at CERN
Cold-expanded pipes
    Used for SPS beam absorbers
    Specific tooling required for each tube diameter
    Not compatible with UHV
    Only straight tubes
    Efficiency unknown
    Very long process
    Issues encountered

## Slide 4: Techniques used for BIDs at CERN (2)
Brazing
    Used for Collimators
    Compatible with UHV
    Quality highly dependant on vendor’s expertise
    Good thermal efficiency

## Slide 5: Techniques used for BIDs at CERN (3)
Clamping
    Used for TIDVG#4 (previous SPS beam dump 2017-2018)
    Compatible with UHV
    Sensitive to machining precision
    Dependent on contact pressure
    Efficiency low (unquantifiable)

## Slide 6: Heat transfer through interface
Mechanical contact
Brazing
Diffusion bonding

## Slide 7: Good bonding…

## Slide 8: Diffusion Bonding by HIP
Hot Isostatic Pressing (HIP)
    High temperature (typically up to ~1400ºC with Mo heaters or up to ~2000ºC with Gr heaters) → promoting diffusion
    High pressure (up to ~200 MPa) → limiting grain growth
    Inherently “clean” process (under Argon)
    Compatible with UHV (inner porosity removed)
    Reproducible results
    Maximum thermal efficiency (thermal resistance at interface virtually removed)

## Slide 9: Diffusion Bonding R&D and Applications at CERN
Two General Categories
Cuprous & SS
P ~ 100 MPa
T ~ 950 ºC
Refractory metals
P up to 200 MPa
T up to 1400 ºC
Cu-OFE
CuCr1Zr
ODS Cu
316L/304L
W
Ta, Ta2.5W
TZM
Nb, Nb1Zr, Nb10Hf1T1

## Slide 10: Cuprous Materials – Stainless Steel
First Tests

## Slide 11: Microscopy
  Observations
  No discontinuities at SS/Cu interface
  No defects detected by PT
  Grains across Cu/Cu interface
SEM Images
SS
CuCrZr
CuCrZr
CuCrZr

## Slide 12: Thermal conductivity across interfaces
From the thermal point of view the bonding is “PERFECT”

## Slide 13: Mechanical Characterisation

## Slide 14: Application 1: SPS Dump
21/01/2019
14
Seamless tube inside vacuum
2500mm-long plate

## Slide 15: SPS Dump
Successful installation of dump in readapted caverns in SPS LSS5

## Slide 16: Full-Scale Prototype
1
2

## Slide 17: Real Behaviour
PROTOTYPE TEST
84 KW
(Pianese et al. https://doi.org/10.1103/PhysRevAccelBeams.24.043001)
OPERATIONAL EXPERIENCE OF REAL DUMP
BEAM POWER = 100 KW
see poster ID 118

## Slide 18: Application 2: PS Internal Dump

## Slide 19: PS Internal Dump Construction
AFTER HIP
BEFORE HIP
alumina coating (no bonding)
coated blocks removed after HIP

## Slide 20: HIP without capsule – Prototype
CUCr1Zr
S. Steel
EBW
Explosion bonding
TIG
Before HIP
Cuts after HIP – Perfect bonding

## Slide 21: Refractory metals
Preliminary investigations (2016)
HIP: 200 MPa / 1200 ºC

## Slide 22: Refractory Metals – Extensive R&D
HIP
150 MPa
1200 ºC
HIP
200 MPa
1400 ºC
Main Observations
Bonding achieved in all interfaces apart from W/W and TZM/TZM
Bonding of TZM/W achieved only for High P&T HIP
Interface thermal resistivity removed in all cases
Mechanical strength of bonding is better for higher P&T HIP
Details in Busom Descarrega et al.
https://doi.org/10.1002/mdp2.101

## Slide 23: Alternative cladding materials – Nb alloys
HIP Parameters
P = 200 MPa
T = 1200 ºC
1400 ºC
Non-trivial procurement of Nb alloys (particularly C103).
Nb alloys tend to show inhomogeneous microstructure.
All Nb alloys successfully plastically deformed.
Virtually no thermal contact resistance for all combinations of materials.
Preliminary (fresh) results of the interface tensile tests show higher strength for Nb-TZM than for Nb-W

## Slide 24: Application: BDF Target
High thermal power (300 kW) → cooling needs
High POT → radiation damage
Slow extraction but high spill power density → Quasi-static thermal-induced stresses
TZM & W core Target as reasonable physics & engineering compromise. Ta2.5W HIPed cladding (Baseline design)
13 x TZM blocks (580 mm)
5x W blocks (780 mm)
1.5 mm
⌀250 mm
25-350 mm
Ta2.5W cladding
Baseline beam parameters of the BDF Target operation. https://doi.org/10.23731/CYRM-2020-002
https://doi.org/10.1103/PhysRevAccelBeams.22.113001
BDF Target water cooling layout (20bar, 5m/s)
~ 4.0×1019 p+/y
See JL Grenard’s and C. Ahdida’s presentations on Friday

## Slide 25: BDF Target – Alternative designs
TZM
W
W
TZM
W
W
TZM
Cu

## Slide 26: Irradiation tests at CERN – BDF Target Prototype

## Slide 27: BDF Target Prototype removal (2020)

## Slide 28: BDF Target Prototype removal (2020)

## Slide 29: BDF Target Prototype – PIE

## Slide 30: Conclusions
Diffusion bonding provides excellent thermal/structural performance of the interfaces for several materials
Maximum cooling efficiency can be obtained in BIDs thanks to this technique
Reproducible results for a given set of parameters
UHV compliant
Extensive operational experience from different institutes