## Slide 1: Present design status of COMET target at J-PARC
J-PARC, KEK
Shunsuke Makimura
High power targetry workshop 2023
at riken on 8th nov. 2023
COMET Phase alpha target from pion transport beamline

## Slide 2
Neutrino [n]
He-cooled graphite
Muon [MLF-MUSE]
Rotating Graphite
Neutron [MLF]
Liquid Mercury
Hadron [HEF]
Water cooled gold/ high-Z rotating target
Graphite (P1), W (P2) [COMET]
2
COMET target at J-PARC
J-PARC Main Ring
South experimental hall in Hadron facility

## Slide 3: COMET target & MLF muon target ( MLF: Materials and Life Science experimental Facility )
COMET target: Search for mu-e conversion
Located in high magnetic field to transport as large number of pions/muons as possible. Large Acceptance. Difficult to disperse the beam loss.
 | MLF target (Conventional) | COMET P1 | COMET P2
Proton beam | 3 GeV, 1 MW | 8 GeV, 3.2 kW | 8 GeV, 56 kW
Beam sigma | 3.5 mm | H: 2.3 mm, V: 2.3 mm | (H: 2.3 mm, V: 2.3 mm)
Target material | graphite | graphite | Tungsten
Target thickness | 20 mm | 700 mm | 160 mm
Beam loss on target | 3.3 kW | 110 W | 7 kW
Time structure | 25 Hz, Double Pulsed, 110 ns | 0.5 s. extraction in 2.5 s. | -
MLF muon target:
Multipurpose use
COMET facility: Y. Fukao
Oral session

## Slide 4: Time structure in COMET Phase 1
energy | 8GeV
power | 3.2 kW
proton / bunch proton / spill | 1.6 x 107 6.2 x 1012
cycle extraction | 2.5 sec. 0.5 sec.
J-PARC
Case: COMET Phase1
Bunched Slow Extraction
Extraction: 0.5 sec.
Time (s)
P-Intensity (a.u.)
2.5 s
0.5 s
Case: Phase2
Proton beam intensity: 56 kW

## Slide 5: Engineering Run: Phase alpha
Beam loss monitor
Coincidence measurement
Extinction monitor & beam window
Phosphor plate & imaging tube camera
3D-printed beam window
Y. Nagasawa in poster session
Pi - production target
C/C composite, t=1.1 mm
Transport of Proton beam w/o the capture solenoid magnet
Studies for secondary particles transport & detection
Operation in Feb. 2023

## Slide 6
Pion production target for phase 1
Manufacturing of target support by C/C composite
The objective is to collect as many muons as possible.
Target support
Should not disturb the pion transport
Will be irradiated by proton beam
Material & Structure
Refractory material
Not-bulk material
Low-density is preferable
C/C composite
SS304, 64Ti, Inconel
Graphite rod, L=700 mm, is floating on the center of superconducting solenoid magnet.
Reinforcement of target support for the axial direction
6

## Slide 7: Dose analysis, Thermal analysis & Eddy current analysis
Max. temperature: 200 °C
PHITS & ANSYS simulation by Metal technology Co., LTD.
Proton distribution on upstream view
Residual radiation dose analysis by Kyusyu University
Eddy current analysis when the quench occurs by Sumi in Cryogenic section
7

## Slide 8: Target assembly in phase 1
The target assembly is inserted into the solenoid shield by semi-remote-handling.
3000 kgf of load by the air-pressure of pillowseal must be considered.
We must consider
How the structural strength is guaranteed.
How the accuracy is guaranteed.
How it is maintained in the high radiation area.
Maintenance with local shielding
8

## Slide 9: Beam profile monitor on target position
9
Collaboration with Hong Ming & Liang Wen in Institute of Modern Physics in China
Profile measurement ＠CAFÉ Linac, IMP
Profile image is transported through mirror and optical fiber.
Side view
Proton beam twines around the axis of solenoid magnetic field.
Downward 40 cm on the dump position
Difficult to align the beam position on target
Importance of beam profile monitor on target position.
Target position
Fluorescent material, Al2O3+Cr2O3 coating on graphite.
The image is transported by optical fiber.
Originally developed at ORNL for SNS measurement

## Slide 10: COMET Phase 2 target
The higher density of target material, the lower spatial volume of muon source
The lower spatial volume, the higher capture and transport efficiency of muon
 | graphite | tungsten
Density (g/cc) | 1.82 | 19.2
Transport efficiency | 1 | 3
COMET | Proton beam power | Target material | Cooling
Phase 1 | 3.2 kW | Graphite | Thermal radiation
Phase 2 | 56 kW | Ta-clad Tungsten | Water cooling
Mu2e@Fermi | Proton beam power | Target material | Cooling
Phase 1 | 8 kW | Tungsten | Thermal radiation
Water cooling Ta-cladding tungsten target at RAL
Thermal radiation cooling tungsten target at Mu2e
Design & Fundamental Research: US-JP collaboration with Fermi-lab is under discussion.
10
TFGR tungsten: S. Makimura
He-embrittlement: T. Sakamoto
Water-cooling target: N. Kamei
Poster session
Oral session

## Slide 11: Summary
Thanks for your attention
11
The developments of the COMET target, located on the center of solenoid magnetic field.
Phase alpha operation in Feb, 2023
Design of Phase 1 is on going.
Development for Phase 2 will start soon.

## Slide 12: Target assembly in phase 1
Recent update:
The plug shield is necessary to decrease the residual radiation dose of the D.S. flange through PHITS simulation
Cantilever beam structure
The distortion of the target position is 2-3 mm due to the weight of the inner collimator, 50 kg.
The target assembly is inserted into the solenoid shield.
3000 kgf of load by the air-pressure of pillowseal must be considered.
We must consider
How the structural strength is guaranteed.
How the accuracy is guaranteed.
How it is maintained in the high radiation area.

## Slide 13: Accuracy and precision
Difficult to use guide pins because of the limitation of the space and the risk of the stuck here.
The weight of the plug shield is just supported by the inner collimator.
Plug shield
Inner collimator
Need the space for guide pins
Two horizontal guide pins and two planes determine the accuracy and precision.
Two long holes against the pins on D.S. flange.
6 screws integrate the fixing plate of the target assembly with the D.S. flange.

## Slide 14: structure Against load of pillowseal and semi-remote maintenance
3000 kgf of load by the air-pressure of pillowseal
Shaft structure on the center position of the load
The location of the target assembly can be adjusted against the fixing plate by the adjustment arm. The plug shield is just supported by the inner collimator.
Inner collimator
Plug shield
Adjustment arm
Fixing plate
Shaft structure
The position of the target assembly can be adjusted, and 6 screws can be fixed on the top of iron yoke that is low radiation area.