## Slide 1: Microstructures, strengths of Al6061-T6 after irradiation in SINQ Target-13
HPTW2023, RIKEN, Wako, Japan 09.11.2023
Peng Song, Yong Dai (PSI), Hossein Sina, Michael Wohlmuther (ESS)

## Slide 2
Content
Backgrounds & Objective
Material & irradiation conditions
Results
Microstructures before irradiation
Microstructures after irradiation
Tensile test results
Ⅳ. Conclusions

## Slide 3
Materials applied to PBW
Europe Spallation Source (ESS)
Thickness:
< 1.25 mm
Proton Beam Window (PBW)*:
Suffer from high-fluence protons (2 GeV)
Low scattering of proton beam (< 1%)
Thickness less than 1.25 mm
Requirements :
Good radiation tolerance
Good thermal conductivity
Light atoms
Good strength
Background
Al alloys:
Al6061-T6 for ESS (5 MW)
AlMg3 for SINQ (1.4 MW)
Al5083 for MLF (1 MW)
Max. p-fluence: 8.6×1025 p/m2 Max. 8.5 dpa
AlMg3
*R. Vivanco, et al. IOP Conf. Series: Journal of Physics: Conf. Series 1021 (2018) 012065
Notes: The PBW (Proton Beam Window) is the device in charge to separate the ultra-high vacuum atmosphere of the accelerator, to the rough vacuum atmosphere present at target side.

## Slide 4
Radiation-induced changes in tensile properties of Al alloys*
Objective: Microstructures of Al6061-T6 after neutron or proton irradiation?
Radiation-induced swelling as a function of Fast fluence
Objective
*Performance of Aluminum in Research Reactors, K. Farrel, Oak Ridge
6061-T6
6061-T6
5052-O
4-9Al
5052-O
Seite 4
Objective
Stress, MPa
Uniform
elongation, %
Swelling, %

## Slide 5
Content
Backgrounds & Objective
Material & irradiation conditions
Results
Microstructures before irradiation
Microstructures after irradiation
Tensile test results
Ⅳ. Conclusions

## Slide 6
wt.% | Si | Fe | Cu | Mn | Mg | Cr | Zn | Ti | Al
Max. | 0.8 | 0.7 | 0.4 | 0.15 | 1.2 | 0.35 | 0.25 | 0.15 | Bal.
Chemical Composition
Material:Al6061-T6
Thermal treatments
Possible second phases*
Grain
morphology
General
microstructures
10 μm
200 nm
*Acta Materialia 132 (2017) 209-221.

## Slide 7
Specimen | Irrad. T (°C) | Dose (dpa) | He (appm) | H (appm) | Test T (°C):
7-LT-N20 | ⁓ 62 | 10.1 | 455 | 1095 | ⁓ 32
7-LT-N19 | ⁓ 62 | 10.1 | 455 | 1095 | ⁓ 152
SINQ at PSI
7-LT-N20: As-irradiated
7-LT-N19: Irradiation + annealed (Irrad.+ ann.)
Irradiation conditions

## Slide 8
Content
Backgrounds & Objective
Material & irradiation conditions
Results
Microstructures before irradiation
Microstructures after irradiation
Tensile test results
Ⅳ. Conclusions

## Slide 9
Microstructures before irradiation: big precipitates
Si, Fe (Mn, Cr), Mg, Al
Mg, Si, Al
Z = Al<001>
Al<002>
π-phase Al9FeMg3Si5
⁓ 30 nm

## Slide 10
Needle-shaped
precipitates ⁄⁄ Al <001>
Z = Al <001>
Averaged length: 22.1 ± 10.3 nm Number density: (1.7 ± 0.8) × 1022 m-3
Microstructures before irradiation: Needle-shaped

## Slide 11
pole 110 g = [-1 1 -1]
g200
g200
g220
g220
pole 110 g = [-1 1 -1]
Microstructures after irradiation: general view
Perfect type: ½<110>
Faulted frank type: 1/3<111>
Project plane: fcc Al (110)

## Slide 12
pole 011 g = 11-1
pole 011 g=-200
pole 011 g=-11-1
g/B vectors | 1/2[1 1 0] | 1/2[-1 1 0] | 1/2[0 1 1] | 1/2[0 1 -1] | 1/2[1 0 1] | 1/2[-1 0 1]
[1 1 -1] | 2 | 0 | 0 | 2 | 0 | -2
[-2 0 0] | -2 | 2 | 0 | 0 | -2 | 2
[-1 1 -1] | 0 | 2 | 0 | 2 | -2 | 0
Microstructures after irradiation: loops & precipitates
As-irrad.

## Slide 13
B vectors:
1/3[1 1 1]
1/3[1 1 -1]
1/3[1 -1 -1]
1/3[1 -1 1]
Z = (011)Al
Microstructures after irradiation: faulted frank loops
rel-rod?
As-irrad.

## Slide 14
1.7 ± 0.4 nm
⁓ 2.6 × 1023 m-3
2.5 ± 0.5 nm
⁓ 1.7 × 1023 m-3
Under focus ~ -640 nm
Under focus ~ -750 nm
Microstructures after irradiation: bubbles inside grain

## Slide 15
As-irrad.
Irrad.+ann.
Microstructures after irradiation: bubbles at GBs

## Slide 16
 | As-received @ 22 ℃ | As-received @ 147 ℃ | As-irradiated @ 32 ℃ | As-irradiated @ 152 ℃
Yield stress, MPa | 230 | 230 | 260 | 227
Tensile test results
ε: 10-3 s-1
Obvious loss of ductility
but very small hardening!
•
Eng. strain ε, %
Eng. Stress, MPa

## Slide 17
Conclusions
 |  | Needle-shaped | Small round | Frank loops | Perfect loops
As-received | Size, nm | 22.1 ± 10.3 | 6.0 ± 1.2 | × | ×
 | Density, m-3 | (1.7 ± 0.8) × 1022 | (6.6 ± 4.5) × 1021 | × | ×
As-irradiated | Size, nm | 11.6 ± 3.8 | 4.8 ± 1.9 | 7.9 ± 2.8 nm | 19.7 ± 8.6 nm
 | Density, m-3 | ~4.3 × 1021 | ~9.6 × 1021 | (6.3 ± 1.5) ×1021 m-3 | ~1.0 × 1022
As-irradiated + annealing | Size, nm | 30.8 ± 15.9 | 4.1 ± 0.9 | × | 56 ± 20
 | Density, m-3 | (2.5 ± 0.1) × 1022 | (4.2 ± 0.7) ×1021 m-3 | × | ~9.9×1019
Length distribution of needle-shaped precipitates
Irrad.+ ann.
As received

## Slide 18: Thanks a lot for your attention!

## Slide 19
Discussion
As-received
As-irradiated
Irradiated + annealed

## Slide 20
22.1 ± 10.3 nm
(1.7 ± 0.8) × 1022 m-3
Size distribution of needle-shaped precipitates

## Slide 21
Pole 110
g = [1-11]
3g excited
g = 200
g = 02-2
Microstructures before irradiation

## Slide 22
Al-alloy: Al 6061-T6
Al-alloys for PBW applications
Irradiation in STIP-7 (Target-10, 2013-14)
R4
n-flu. | 9.5x1025/m2
p-flu. | 1.6x1025/m2
Dose | 10.1 dpa
He | 455 appm
H | 1095 appm
Tirr | 62°C
to be finalized
Inconel 718 (for LANSCE, SNS)
Al alloys ( for ESS, SINQ, MLF)
Ti-Al-V alloys
High Entropy Alloys (HEAs)