## Slide 1
3. Commissioning: Ultrasonic Fatigue Rig Methods and Calibration Results
1. Reasons: Beam Window Fatigue Worries
Laser
Line formed corresponding to sample deformation
Sample mounted to vertically oscillating ultrasonic horn and deflects due to inertia
Mirrored surface of sample reflects laser
Chart: N
Failure | 387.0546 | 458.3711 | 484.7379 | 478.382 | 524.6827 | 510.312 | 458.7584 | 484.1741 | 478.1579 | 557.3908 | 400.2453 | 542.8206 | 488.9869 | 587.205 | 449.9738 | 373.8764
Highest Survived Stress | 322.5455 | 381.9759 | 403.9482 | 398.6517 | 437.2355 | 425.26 | 382.2987 | 403.4784 | 398.4649 | 464.4923 | 333.5378 | 452.3505 | 407.4891 | 489.3375 | 374.9781 | 311.5637
Testing Irradiated Titanium Alloys for High-Cycle Fatigue Richard Cowan, Phil Earp, Mike Fitton, Eric Harvey-Fishenden
LBNF 120Gev beam
LBNF Target Upstream Beam Window
2. Samples: Benefits and Irradiation Campaigns
N2 gas
p+
Meso-scale Cantilever
Birmingham Sample Irradiation Environment
Laser strain evaluation
S-N Curve for unirradiated calibration samples
T2K 30 GeV beam
T2K Target Upstream Beam Window
Ultrasonic Fatigue Rig setup description