## Slide 1
Mechanical alloying
in He atmosphere
No ion implantation
No radioactivity
Fabrication of W-1.1%TiC with helium bubbles
via powder metallurgical route
incorporated with helium ambient mechanical alloying
No displacement damage
Bright Field Image
HAADF Image
50nm
He Bubbles
There are no reports on bulk W alloys including only He bubbles.
W alloys with He bubbles were fabricated by MA in He atmosphere.