## Slide 1: 2. Radiation damage in target material and related simulations
Shunsuke Makimura (J-PARC, KEK)
10th November 2023
High Power Targetry Workshop @ RIKEN

## Slide 2
(Invited) ''Overview of Radiation Materials Science and Radiation Damage Modeling'' (David Senor)
(Invited) "Irradiation damage of diamond by ion implantation'' (Masahiko Ogura)
ID90 ''Capabilities of the FLUKA particle transport code for the design and operation of high power targetry systems'' (Francesc Salvat Pujol)
ID22 ''Measurement of displacement cross section for high-energy protons and future plan for material damage using 0.4 GeV protons at J-PARC'' (Shin-ichiro Meigo)
ID70 ''RaDIATE Collaboration Status and Recent Results on Material Studies'' (Frederique Pellemoine)
ID36 ''Novel Materials R&D for Next-Generation Accelerator Target Facilities'' (Kavin Ammigan)
ID47 ''Computational Exploration of High Entropy Alloys as Promising Materials for Future Beam Windows'' (Gaurav Arora)
ID100 ''Evaluation of β-phase based titanium alloys'' (Eiichi Wakai)
The Nick Simos Effect
(Patrick Hurh)

## Slide 3: (Invited) ''Overview of Radiation Materials Science and Radiation Damage Modeling'' (David Senor)
Radiation damage
  Point defects
  Displacement cascade
  Defect annihilation, clustering and mobility
Radiation damage microstructures
  Radiation induced segregation
  Dislocations
  Voids and bubbles
  Phase stability
Macroscopic effects of radiation damage
  Irradiation hardening and embrittlement
  Radiation growth and swelling
  Irradiation creep
  Irradiation assisted stress corrosion cracking
  Transport property degradation
Radiation damage modeling
  Atomic Level Simulations
  Microstructural Modeling
  Machine Learning to Integrate Experiments and Modeling
Was. 2007. FRMS, Springer
Jenkins and Kirk. 2001. Characterization of Radiation Damage by TEM, IOP
Atomic scale
Macroscopic
Modeling

## Slide 4: (Invited) "Irradiation damage of diamond by ion implantation'' (Masahiko Ogura)
Diamond is expected to be applied to next-generation power electronics and quantum sensor
Ion implantation technology is indispensable for realizing diamond devices
The depth and concentration can be controlled by ion energy and dose, respectively.
Irradiation damage is simultaneously introduced, that degrades electronic properties and device performances.
The accumulation of defects induces graphitization and prevents from returning to crystalline diamond.
As for the doping technique, boron, the most promising p-type dopant, was successfully ion-implanted to show p-type characteristics from an early stage, although sufficient electronic properties for device applications have not yet been achieved.
Clear n-type properties have not been shown by ion implantation. A key issue is how to eliminate the influences of irradiation damage.
Point defects by ion implantation can be effectively utilized. For example, Quantum sensing devices using magnetic resonance related to the vacancy complexes with additive elements such as nitrogen (N-V center) in diamond. Here, it is necessary to control the position so that a vacancy should be located next to an ion-implanted additive element.

## Slide 5: ID70 ''RaDIATE Collaboration Status and Recent Results on Material Studies'' (Frederique Pellemoine)
In-Beam Studies
Evaluate in-beam performance of candidate materials
Irradiated Material Studies: high energy proton irradiation at BNL-BLIP
Thermal shock testing: HiRadMat facility at CERN
Alternative Methods
Emulate high energy proton irradiations for accelerated and cost-effective material screening
Low Energy Ion: for assessing radiation damage effects
Electron beam for thermal shock and fatigue testing
Novel Testing Methods (fatigue studies)
Novel Target Materials
New materials with enhanced thermal shock and radiation damage resistance
High-Entropy Alloys
Nanofibers
Composite materials
Heat treatment
Develop Modeling
Prediction of fundamental response of various materials to irradiation and thermal shock
Helium gas bubbles formation and segregation
Radiation damage effects
Heat transfer mechanism in nanofiber media
RaDIATE collaboration created in 2012, with Fermilab as the leading institution. The collaboration has grown up to 20 institutions over the years.

## Slide 6: (Materials)
ID36 ''Novel Materials R&D for Next-Generation Accelerator Target Facilities'' (Kavin Ammigan)
ID100 ''Evaluation of β-phase based titanium alloys'' (Eiichi Wakai)
  High-Entropy Alloys (for beam windows)
SEM images of Zirconia nanofibers produced at Fermilab, (a) bulk nanofiber mat, (b) single nanofibers revealing polycrystalline grains (S. Bidhar)
Electrospinning technique and Taylor cone.
Intrinsically tolerant to both thermal shock and radiation damage
  Nanofiber Materials (secondary particle-production targets)
HEAs are alloys with multiple principal elements:
Large composition space to explore new materials
Sectioned arc-melted ingots (UW-Madison)
No observable cracks at corners of indents
4 HEA compositions
Cr33Mn33V33
Cr31Mn31Ti7V31
Al15Cr20Mn20Ti10V35
Al15Co4Cr25Mn15Ti6V35
Displacement Damage | Phenomena
0 dpa | High number density Precursor does not act as sink, but as decreasing of diffusion velocity of point defects
3 dpa | High number density: Omega like embryo formation and it can act as sink site
6 dpa | High number density: omega like embryo is developing
9 dpa | Disappearing of omega-like embryos
11 dpa | Disappearing of omega-like embryos and precursors
β-Ti-15Cr-3V-3Al-3Sn alloy (ST and STA)
Ion irradiation 11 dpa, R.T.
Nano-hardness
TEM observation
TEM diffraction pattern & HREM & Positron Annihilation Measurement
Precursors & Omega-like embryo

## Slide 7: ID47 ''Computational Exploration of High Entropy Alloys as Promising Materials for Future Beam Windows'' (Gaurav Arora)
Density functional theory (DFT)
Work on the principle of quantum physics
Highly accurate
Computationally expensive
Limited to ~300 atoms
Software: VASP, Q-espresso, etc.
Molecular dynamic (MD)
Work on the principle of Newton laws
As accurate as interatomic potentials
Computationally cheap
Million of atoms can be modeled
Software: LAMMPS
Development of accurate interatomic potentials is the key challenge in designing or studying defect properties of materials
High-Entropy Alloys
CALPHAD stands for "Calculation of Phase Diagrams.“
Approximately 600 simulations are performed for each composition.
Forces and energies are extracted and fed into making of machine learning potential.
Preliminary results
Model can predict energies accurately
Increasing model complexity decreases the error

## Slide 8: Modeling
ID90 ''Capabilities of the FLUKA particle transport code for the design and operation of high power targetry systems'' (Francesc Salvat Pujol)
ID22 ''Measurement of displacement cross section for high-energy protons and future plan for material damage using 0.4 GeV protons at J-PARC'' (Shin-ichiro Meigo)
Energy (dose) deposition
Secondary particle production
Radiation damage estimates
  DPA (DPA-NRT and ARC-DPA)
  H and He production
Radiation to electronics
Prompt radiation and activation
  Prompt and delayed in a single run
  Radionuclide inventories
  Ambient doses
Provides input for finite element analyses (ANSYS)
BLIP gas production
Application:
radiation damage in the Muon Collider arc
neutron attenuation benchmark
CERN Shielding Benchmark Facility (CSBF)
dpa (displacement per atom)：
Widely used as damage index for fission
and fusion reactors, and accelerator fac.
dpa = Fluence x displacement X-sec
Lack of data above 20 MeV: Difficult validation of calculation models
⇒ Experiments at J-PARC, FNAL
Applicability should be confirmed for further higher energy (i.e., Ep 440 GeV).
Experiments at HiRadMat, CERN in 2025