## Slide 1: TOMOYA KAto
RIKKYO UNI

## Slide 2: Radiation Hardness of micro-coaxial cable

## Slide 3: Structure of μ-Coax
https://www.i-pex.com/ja-jp/library/video/micro-coaxial-capabilities
テフロン
Weak against Radiation
引用:https://www.i-pex.com/ja-jp/library/video/micro-coaxial-capabilities
直径0.24mm
Teflon
Teflon
https://www.osti.gov/servlets/purl/1467983

## Slide 4: Relative Locations
1010
/cm2
Try to estimate radiation dose at INTT m-coax positions by scaling from Asai’s paper.
Collision Point
3 years of sPHENIX operation
1.5×1011
/cm2
How much radiation does sPHENIX expose you to in 3 years of operation?
Radiation Damage Study for PHENIX Sillicon Stripixel Sensor ([18] J. Asai, et al., arXiv:0710.2676)
PHENIX Asai’s paper
Run6 p+p
Beam Line

## Slide 5: Unit conversion to compare with existing radiation hardness data
PFA is a derivative of PTFE
1.5×1011/cm2 (1 MeV Neutron Equivalent) into Gy

## Slide 6: Unit conversion from Neq to Gy via Sv
Equivalent dose (Sv) = radiation weighting factor (20) × absorbed dose (Gy)
https://www.icrp.org/docs/P116_Japanese.pdf
The number of neutrons in sPHENIX is 1.5
2.3
https://www.osti.gov/servlets/purl/1467983

## Slide 7
https://www.icrp.org/docs/P116_Japanese.pdf

## Slide 8
2.3

## Slide 9: Does neutron irradiation change PFA?

## Slide 10: What is RANS?
RANS is Neutron irradiation system in Riken.
BerylliumBe
Proton
Neutron
IonSourceH+

## Slide 11: Irradiation Attempts @ RANS
Run-I (March, 2022)
  Pilot run with prototype cable and PFA samples
  Mechanical test of PFA
Run-II (November, 2022)
  Real run with production cable
  Electrical property test

## Slide 12: The number of neutrons irradiated
sPHENIX
1.5×1011/cm2
2.3
neutrons irradiated in RANS
4.9×1011/cm2
7.4
<
RUN1

## Slide 13: Radiation Damage
Before
After
No obvious damage in PFA samples

## Slide 14
We irradiated more neutrons than sPHENIX, but no obvious change in PFA material!
No electrical effects?
Let's measure the signal transmission performance!

## Slide 15: signal transmission performances
non-irradiated μ-coax
neutron- irradiated μ-coax
Compare the signal transmission performances with/without irradiation
TDR
(Time Domain Reflectometry)
S-parameters
①transmission loss
②return loss
Eye Pattern

## Slide 16: Neutron irradiation in RANS

## Slide 17
Prepare three types of micro coaxial cables For 1-hour, 2-hour, and 3-hour exposure

## Slide 18: Result
sPHENIX 3years
24years
51years
78years in terms of sPHENIX
irradiated the number of neutrons
> sPHENIX's the number of neutrons
Amount of neutrons irradiated using RANS
the amount of radiation μ-coax will be exposed to
at sPHENIX at around the conversion cables are installed.
1.5E+11
12.4E+11
26.3E+11
39.9E+11
RUN2

## Slide 19: transmission performance measurement results

## Slide 20: TDR (Time Domain Reflectometry)
Purpose : to measure the impedance characteristics of a transmission line
①send a short electrical pulse(800ps) down the transmission line
②the reflection that is created when the pulse encounters a change in impedance
③observe the reflection
①800ps
②Change in impedance
③

## Slide 21
①800ps
②Change in impedance
③
③observe the reflection and time delay
the time delay between the transmitted and reflected signals is used to determine the distance to the impedance change.
ZL: impedance of the sample
Z0: known impedance
ｐ=reflected voltage/input voltage

## Slide 22: Result of TDR
Results are consistent within 5%. May be induced by individual difference of the harnesses.

## Slide 23: s parameter
s para＝
＝ transmission loss
Apply the input signal
Signal source
measure

## Slide 24: Result of transmission loss
Vertical axis: dB = 20LOG10(S) / Horizontal axis: Frequency of input signal
Good
Bad
Micro coaxial cable has S = -0.99±0.02dB at 0.2GHzThat is, signal attenuation is (89±2)% of the original
In actual use
Results are consistent within 2%.
May be induced by individual difference of the harnesses.

## Slide 25
Good
Bad
0hour
1hour
2hour
3hour
Results are consistent within 4%.
May be induced by individual difference of the harnesses.
Result of Return loss

## Slide 26: Result of Eye Pattern
→No abnormality (change) in waveform
5ns
800mV
Eye pattern is created by cutting various transmission signals bit by bit and overlapping them

## Slide 27: Calibration test results

## Slide 28: Calibration pulse test was performed using μ-coax irradiated with neutrons.
μ-coax has three harnesses (J3, J4, J5).
Features.
J3 is a RESET signal and data line
J4 is data line only
J5 is BCO, SC, CLK and data lines

## Slide 29: measurement item
Four types of measurements were made
J3:0H
J4:3H neutron- irradiated
J5:0H
J3:3H neutron- irradiated
J4:0H non-irradiated
J5:0H non-irradiated
J3:0H
J4:0H
J5:3H neutron- irradiated
J3:2H neutron- irradiated
J4:1H neutron- irradiated
J5:3H neutron- irradiated

## Slide 30: Result
Four types of measurements were made
J3:0H
J4:3H neutron- irradiated
J5:0H
J3:3H neutron- irradiated
J4:0H non-irradiated
J5:0H non-irradiated
J3:0H
J4:0H
J5:3H neutron- irradiated
J3:2H neutron- irradiated
J4:1H neutron- irradiated
J5:3H neutron- irradiated
No abnormality in all

## Slide 31: Conclusion
PFA material No effect of irradiation
TDR ,s parameter, Eye pattern No effect of irradiation
Calibration pulse test No effect of irradiation
Based on above results, we conclude the radiation hardness of m-coax is sufficient for 3 years of operation in sPHENIX

## Slide 32: SUB

## Slide 33: How much radiation does sPHENIX expose you to in 3 years of operation?
Radiation levels have been measured in the PHENIX experiment (previous experiment)
1010
/cm2
PHENIX
Actual measured value
sPHENIX
μ-coax
1.5×1011
/cm2
Compare experimental conditions
(1 MeV Neutron Equivalent)
参考文献:Radiation Damage Study for PHENIX Sillicon Stripixel Sensor ([18] J. Asai, et al., arXiv:0710.2676)

## Slide 34
https://www.icrp.org/docs/P116_Japanese.pdf

## Slide 35: Radiation Hardness of Fluoropolymer
https://www.osti.gov/servlets/purl/1467983
BEX
HDI
m-Coax
hard
In general, fluoropolymer is known to to be weak against the radiation
Dielectric material
sPHENIX3年
5kGy
?
Torn into pieces?

## Slide 36: Method : How to examine the radiation hardness
non-irradiated μ-coax
neutron- irradiated μ-coax
Compare
・the signal transmission performances with/without irradiation

## Slide 37: どれぐらいの放射線量ですか？
等価線量(Sv)=放射線加重係数(20)×吸収線量(Gy)
https://www.icrp.org/docs/P116_Japanese.pdf
sPHENIXの中性子数は1.5
https://www.osti.gov/servlets/purl/1467983

## Slide 38: Estimate the number of neutron

## Slide 39: How to examined radiation hardness of the μ-coax-cables
① Measure high speed signal transmission performance of the micro-coax cable.
②Calculate the amount of radiation μ-coax will be exposed to at sPHENIX
③ Irradiate neutrons to the micro-coax cable at RANS facility.
④ Redo the measurement of 1 and see if there is any degradation in the performance

## Slide 40: The number of protons in μ-coax
 | protons | neutrons
Existing | 3.59E+17 | 5.47E+11
M-Coax 1hour | 8.39E+17 | 12.4E+11
2hours | 17.2E+17 | 26.3E+11
3hours | 26.1E+17 | 39.9E+11
ratio
ratio
Expected sPHENIX-neutrons =1.5E+11

## Slide 41: Result of TDR
time delay (ns)
Distance (cm)

## Slide 42: how it works
Neutron flux is not the direct observable
↑Measure γ count

## Slide 43: how it works
Neutron flux is not the direct observable
estimate Neutron indirectly from the total charge of proton beam.
↑Measure γ count

## Slide 44: how it works
Neutron flux is not the direct observable
estimate Neutron indirectly from the total charge of proton beam.
The neutron flux can be calculated by
1.cross calibrating proton charge
2.gamma ray emission from an indium foil
↑Measure γ count

## Slide 45
 | Number of protons | Number of γ rays | number of neutrons(Neq)
Existing Measurement | Known | known | Calculate 5.4E+11
INTT | Measured |  | Goal
Number of protons = time ×(average I) /e
Number of γ rays that measured by Ge detector
e =1.62E-19
ratio
Existing Measurement : Courtesy of Ms. Hatsuda,
Juntendo University
ratio
Neq is the equivalent flux of 1meV neutrons
Number of protons is known from charge of proton beam

## Slide 46: sPHENIXの３年間の稼働でどれぐらい放射線を浴びるの？
PHENIX実験（前実験）では放射線量が実測されている
1010
個/cm2
PHENIX実験の
実測値
sPHENIX実験のマイクロ同軸ケーブル
1.5×1011
個/cm2
実験条件
を比較
中性子線量当量
(1 MeV Neutron Equivalent)
参考文献:Radiation Damage Study for PHENIX Sillicon Stripixel Sensor ([18] J. Asai, et al., arXiv:0710.2676)

## Slide 47: Relative Locations
1010
/cm2
r
z
Asai et.al.
INTT
m-coax
Try to estimate radiation dose at INTT m-coax positions by scaling from Asai’s paper.
Collision Point
Beam Line
Run6 p+p
3 years of sPHENIX operation
1.5×1011
/cm2
How much radiation does sPHENIX expose you to in 3 years of operation?
10,

## Slide 49
Run6 p+p
Delivered Luminosity: 12/pb (50days)
Number of Equivalent Neutrons: 1010/cm2
(1 MeV Neutron Equivalent)
Location: R=10cm, z=25cm, h=1.65
Z=41cm, 42/pb
R=10 cm
9260*R-1.788
[18] J. Asai, et al., arXiv:0710.2676.
Reflection from nose cone